Ordered Structure with Large Periodicity in Polydisperse Ethylene-α-Olefin Block Copolymers

Sheng Li* and Richard A. Register

Department of Chemical Engineering, Princeton University

Session 1, Talk 4 (10:00 AM)

In semicrystalline block copolymers, formation of solid-state morphology can be driven either by block incompatibility or by crystallization of one or more of the blocks.  Depending on the block interaction strength, a wide array of solid-state morphologies may be observed, ranging from spherulitic to confined crystallization within preexisting microphase-separated domains [1,2].  Dow Chemical has recently developed a novel chain shuttling polymerization process to produce olefin block copolymers with alternating amorphous and semicrystalline chain segments, where each block exhibits the most probable distribution [3,4].  We examined the melt and solid-state morphologies of these novel block copolymers, having a high octene content in the amorphous block, using two-dimensional synchrotron small-angle and wide-angle x-ray scattering on specimens oriented by channel die compression.  Diblock copolymers with near-symmetric compositions showed well-ordered lamellar structures at room temperature with long period exceeding 100nm, with little dependence on thermal history, indicating the presence of a microphase-separated melt which templates crystallization.  Furthermore, increasing the polydispersity index of a block copolymer system was found to result in a substantial increase in its microdomain spacing.  Based on the structural and molecular weight information obtained, a qualitative scaling relationship was constructed for the polydisperse olefin diblock copolymers.

[1]	I. W. Hamley, Adv. Polym. Sci., 148, 113 (1999).

[2]	Y. L. Loo, and R. A. Register, Development in Block Copolymer Science and Technology, Chichester, John Wiley & Sons, LTD, 2004.

[3]	D. J. Arriola, E. M. Carnahan, P. D. Hustad, R. L. Kuhlman, and T. T. Wenzel, Science, 312, 714 (2006).

[4] 	P. D. Hustad, R. L. Kuhlman, D. J. Arriola, E. M. Carnahan, and T. T. Wenzel, Macromolecules, 40, 7061 (2007).